SP3020 (07-22-10)

SECTION 03020 - EROSION MATERIALS

(Follow all instructions.  If there are no instructions above a subsection, paragraph, sentence, or bullet, then include them in the project but make necessary modifications to only include project specific specifications.  Delete specifications that do not apply to the project.)

Section 03020, which is not a Standard Specification, is included in this Project by Special Provision.

Description

03020.00  Scope - This Section includes the requirements for erosion control materials.

Materials

03020.10  Commercially Manufactured Compost - Furnish commercially manufactured compost that:

Is processed through thermophilic composting meeting the EPA's definition of "Process to Further Reduce Pathogens".

Is from a commercial compost facility that holds a current DEQ composting permit or is registered with DEQ as a composting facility.

Meets the requirements of the US Composting Council (USCC) and it's Seal of Testing Assurance (STA) program.

Contains a minimum 65% by volume of the following recycled plant waste:

Source-separated yard and garden wastes

Wood wastes

Agricultural crop residues

Wax-coated cardboard

Preconsumer vegetative food wastes

Other similar source-separated materials that the DEQ has determined to have a comparable low level of risk in hazardous substances, human pathogens, and physical contaminants.

Manure or biosolids based composts when approved.

Meets the following compost particle size and media parameters:

| Compost Particle Size |
| --- |
|  | Compost Type |
| Sieve Size | Fine* | Medium* | Coarse** |
|  | Minimum Percent Passing (By Dry Weight) |
| 3" | 100 | 100 | 100 |
| 1" | – | 90 | 90 |
| 3/4" | – | 65 | 70 |
| 5/8" | 95 | – | – |
|  | Maximum Percent Passing (By Dry Weight) |
| 1/4" | – | 50 | 30 |
| * maximum 3 inch particle length ** maximum 6 inch particle length |

| Media Parameters |
| --- |
| Test | Test Method | Requirements |
| Physical Contaminants* | TMECC** 03.08-A | Less than 1.0% |
| Organic Matter | TMECC** 05.07-A | 35% (Minimum) |
| pH | TMECC** 04.11-A | 6.0 to 8.5 |
| Soluble Salt Concentration | TMECC** 04.10-A | 5 dS/m (Maximum) |
| Total Carbon Total Nitrogen | TMECC** 04.02-D TMECC** 04.02-D | Carbon/Nitrogen Ratio |
|  |  | Fine | Medium & Coarse |
|  |  | <25:1 | n/a |
| Stability | TMECC** 05.08-B | 8 or below |
| Maturity | TMECC** 05.05-A | 80% or Greater |
| Moisture Content | TMECC** 03.09-A | 35-60% (Wet Weight) |
| * Man-made Inert ** Test Methods for Evaluation of Compost and Composting |

03020.90  Acceptance - Acceptance of commercially manufactured compost material will be the following:

Quality compliance certification according to 00165.35.

Copies of STA lab analysis.

Copy of DEQ permit or registration of the compost producer.