SPECIAL NOTE FOR UNSEALED JPC PAVEMENT

AND SHOULDER JOINTS

This Special Note will apply when indicated on the plans or in the proposal.  Section references herein are to the Department’s 2012 Standard Specifications for Road and Bridge Construction.

1.0	DESCRIPTION.  This Special Note will only apply to concrete pavements placed on a drainage blanket.  The Department will allow contraction and construction joints with a joint width of 1/8-inch to be left unsealed. Construct all other pavement joints according to the standard specifications.  Seal expansion joints according to the standard specifications.

2.0	CONSTRUCTION.  Saw the joints in a timely manner in order to control cracking. When using a conventional saw, cut joints to a depth equal to 1/3 of the pavement thickness (T).  When using an early entry saw, cut joints to a depth equal to 1/3 of the pavement thickness (T) to a maximum of 3-inches.  Do not bevel the edge of the sawed joint.  Keep joints clean and free of saw cuttings.

3.0	MEASUREMENT AND PAYMENT.  The Department will not measure for payment any work associated with this Special Note and will consider it incidental to the bid item(s) JPC Pavement and JPC Shoulders.

June 15, 2012