SPECIAL NOTE FOR ACCEPTANCE OF DENSITY                                                      OF LONGITUDINAL JOINTS IN ASPHALT SURFACE PAVEMENTS

This Special Note will apply when indicated on the plans or in the proposal.  All applicable portions of the Department’s 2012 Standard Specifications for Road and Bridge Construction apply unless specifically modified herein.  Section references herein are to the Department’s 2012 Standard Specifications for Road and Bridge Construction.

1.	DESCRIPTION.  This note specifies an increased level of compaction for density acceptance testing required for the longitudinal joint of asphalt surface mixtures compacted under Option A requirements.  Due to the inherent difficulty of compacting longitudinal joints, conventional methods of compaction may not be adequate to achieve the desired level of density.

2.	MATERIALS AND EQUIPMENT.  Reserved.

3.	CONSTRUCTION.	 Reserved.

4.	MEASUREMENT.	Reserved.

5.	PAYMENT.

  - Lot Pay Adjustment.   Contrary to Subsection 402.05.02, the Department will use the following Lot Pay Adjustment Schedule to assign pay values for Joint Density within each sublot.

| JOINT DENSITY |
| --- |
| Pay Value | Test Result (%) |
| 1.05 | 92.0-96.0 |
| 1.00 | 90.0-91.9 or 96.1-96.5 |
| 0.95 | 89.0-89.9 |
| 0.90 | 88.0-88.9 or 96.6-97.0 |
| 0.75 | < 88.0 or > 97.0 |

June 15, 2012