SPECIAL NOTE FOR PACKAGED, RAPID-HARDENING

MATERIALS FOR CONCRETE REPAIRS

Use cementitious materials for rapid repairs to hardened hydraulic-cement concrete pavements and structures conforming to ASTM C 928.  The Department will allow but not require the inclusion of aggregate in packaged, dry, mortar material.

Furnish a Certificate of Compliance with each shipment that includes the following:

- Verification that the materials were tested according to ASTM C 928.

- States the actual test results for each requirement.

- State that the test results comply with the requirements.

The Department may sample and test the material furnished at any time.  The Department will reject material not conforming to ASTM C 928 or contained in broken packages.

# June 15, 2012