1N

SPECIAL NOTE FOR PERMANENT, RAPID-HARDENING

CONCRETE PATCHING

Use either of the following fast-setting cementitious materials, or approved equal, for permanent repair of hardened hydraulic-cement concrete pavements and structures.

1)	SET-45, as produced by BASF Construction Chemicals (Master Builders) 23700 Chagrin Boulevard, Cleveland, Ohio 44122-5554

2)	RAPID SET DOT REPAIR MIX, as produced by CTS Cement Manufacturing Corporation, 11065 Knott Avenue, Suite A, Cypress, CA  90630

For materials to be considered an equal, furnish a Certificate of Compliance that includes the following:

1) Verification that the materials conform to ASTM C 928.

2) Verification that the materials attain a minimum 3-hour compressive strength of 4,500 psi.

June 15, 2012