SPECIAL NOTE FOR CORROSION RESISTANT GUARDRAIL

This Special Note will apply where indicated on the plans or in the proposal.  Section references herein are to the Department’s 2012 Standard Specifications for Road and Bridge Construction.

1.0	DESCRIPTION.  Furnish and install all necessary material for each type of guardrail according to Section 719.

2.0	MATERIALS.

2.1	Shapes and Plates.  Conform to ASTM A 588.

2.2	Fasteners.  Conform to AASHTO M 164, Type 3.

  - W-Beams, W-Beam Terminal Section, and W-Beam End Treatments.  Conform to ASTM A 606, Type 4 and AASHTO M 180 Type IV.  Provide the class the Contract specifies.

  - Posts.  Use timber posts conforming to Subsection 814.04.02.

3.0	CONSTRUCTION.  Do not paint or galvanize.  Handle and store guardrail beams so that the traffic face of these beams, used in a continuous run of guardrail, shows no distinctive color differential.

4.0	MEASUREMENT.  The Department will measure the quantity of each type guardrail according to Section 719.

5.0	PAYMENT.  The Department will make payment for the completed and accepted quantities under the following:

Code	Pay Item											Pay Unit

----		Guardrail - Steel W Bm-SFace CR					Linear Feet

----		Guardrail - Steel W Bm-DFace CR					Linear Feet

----		Guardrail Terminal Section, Type, CR				Each

----		Guardrail End Treatment, Type, CR					Each

----		Guardrail Con To Br End, Type, CR					Each

----		Guardrail Con To Concrete Median Barrier CR		Each

----		Guardrail Con To Shoulder Bridge Pier, Type, CR		Each

The Department will consider payment as full compensation for all work required in this note.

June 15, 2012